

* NO UNPLEASANT ODOR
* RESISTS EFFLORESCENCE
* UNSURPASSED WATER & OIL RESISTANCE
* EXCELLENT AS A PLASTER SEALER
* SAFE TO USE

**PREPARATION**

Always read product label carefully before using. TEST FIRST! Due to differences in materials, always test product in several small inconspicuous areas to determine suitability of product for your use. Surface must be clean, dry, and free of all surface coatings and waxes. To remove permanent sealers, use a high quality stripper. Let plaster finishes dry for 48 hours before applying Stain Shield.

**SPECIAL FEATURES**

Stain Shield is a “state-of-the-art” premium, oil and water repellent sealer. It maintains a “Natural Look” appearance without changing color or adding any sheen while forming a barrier that resists moisture, stains and mildew. Suitable for interior and exterior freeze/thaw areas, vertical and horizontal areas. This product is breathable and does not leave a surface coating. Stain Shield Sealer is VOC compliant.

**FEATURES**

* EASY TO APPLY
* ETCH FREE FORMULA
* ONE FORMULA FOR ALL STONE
* LONG LASTING
* RESISTS MILDEW

Meoded Paint & Plaster • 323-308-2600

* info@meodedPaint.com [www.meodedpaint.com](http://www.meodedpaint.com/)

**STAIN SHIELD**

**SEALER**

Technical Data Sheet

**CONCRETE FINISHES**

* Golmex
* Vega
* Concretta FS

(Not Inside Showers)

**LIMESTONE FINISHES**

* Stucco Lamundo
* Marmorino Tintoretto
* Marmorino Palladino
* Tonachino Firenze
* Lime Wash

**APPLICATION**

Apply generously using a solvent resistant natural bristle brush, sponge, paint roller, sprayer or paint pad. Make sure the product is spread out evenly on the surface. *Allow sealant to soak into the surface.* If applied too heavily, pooling and dripping may occur. Wipe off any excess material to avoid drip marks. **Two coats recommended. Second coat can be applied after 1-2 hours of dry time.**

**Cure Time:** Stain Shield cures in 24 hours. Allow surface to dry for 12 hours, before allowing traffic. Keep surface free from staining materials for 72 hours.

NOTE: Apply when temperature is between 50ºF – 90ºF. Avoid puddling and rundown. If sealant comes in contact with surrounding surface, wipe off. If residue appears, reapply some Stain Shield and buff surface with a clean towel.

**Coverage rate** of Stain Shield Sealer will vary depending on porosity and absorbency rate of surface to be sealed. Temperature and application method will also affect coverage.

**One quart will seal between 80-120 square feet.** In most instances, expense of labor exceeds material cost of sealing project. Do not under apply the product as the labor cost of doing the job twice exceeds the material costs.

**Maintenance:** Surface should be kept clean using a neutral cleaner or stone cleaner, as needed.

**Stain Resistance Tests:** Independent test for staining (CTI- T-72) has shown Stain Shield to be extremely effective against a variety of contaminants on a wide range of surfaces, including marble, quarry tile, limestone, and concrete.

**WARRANTY**

Meoded Paints & Decoration Inc. warrants its products for the purpose in which they were intended for, when applied and used in accordance to manufacturer’s instructions. Meoded’s liability, either expressed or implied, is limited solely to the replacement of this product when proven to be defective and does not include any labor costs or consequential damages. It is the user’s responsibility to determine the safety, toxicity, and suitability of this product.

**PRODUCT DESCRIPTION**

**Meoded Paint & Plaster Stain Shield Sealer** is an exciting “State-of-the-Art” “Natural Look” penetrating sealer for water, oil and stain resistance on all Meoded plaster finishes.

**USES**

Recommended for all absorbent plaster finishes.

**Quality Products**